Wooden tables or pallets for block making machines

WOOD SELECTION

Pallets are made of

Pinus Pinaster, also known as

Maritime or Galician Pine.

All wood is sanded and rushed

on both surfaces.

Mechanical properties of

Pinus Pinaster:

Static flexion resistance: 795 kg/cm².

Module of elasticity: 74.000 kg/cm².

Compression resistance: 400 kg/cm².

ASSEMBLY SYSTEM

We are the only manufacturers who use the double dovetail

system in the assembly of our products. Pallets do not need screw

bars or glue as the double dovetail system ensures the planks are bonded

together, thus favouring the natural dilatation and contraction of the wood,

and avoiding the apparition of cracks on the planks.

This system ensures product  quality and guarantees:

- Pallet without warping.

- Homogeneous vibration in the

- whole surface.

- Shorter vibration time.

- Increased productivity.

- More homogeneous

- production.

- Saving of energy.

Double dovetail system assembly.

By the combination of different

factors like the mechanical properties

of elasticity and hardness of the

Pinus Pinaster and the ideal moisture

level of the wood obtained in our

heater, we can ensure that our Pallets have:

- High resistance and load capacity.

- Greater flexibility of use (less

weight than metal, plastic or

harder wood pallets).

Pallets are produced with boards of a single plank.

LATERAL PLANKS

We have incorporated wider and

rounded planks at the end of the boards, as well.

All these characteristics make the Pallets:

- Strong and reliable.

GALVANIZED PROFILE

Pallets have a galvanized profile of 2 mm thick..

The closing of the profile is made

folding the steel in a rounded way in the heads of the pallets, without

welding them (patented system in all

Europe).

This way we ensure that our

pallets do not hook in the machinery

and in the entry of the block making machine.

Even if this selection process is

more expensive, we consider that a

union in their length may produce a

weak point in the board.

PUNCH POINTS

This way the profile is properly

fixed to the planks and protects the

wood in the heads of the pallets.

Pallets are treated by way of immersion as part of the protection

process. Pallets are plunged in a proprietary preparation (oily and solvent base)

to keep them resistant.

This way the wood is effectively protected from fungi and humidity.

TREATMENTS

Pallets have six punch points (three on each side) hydraulically produced on the galvanized profile.

Our quality control is  ISO 9001/2000

Certification accredited in 2005.

Is aware of the importance of the environment and endeavours through its production methods to help guarantee the

conservation of the forests.

For this reason we obtained the Chain of Custody Certification,

which guarantees that our wood comes from forests managed in a

sustainable way.

CERTIFICATIONS

has, as always, its main objective as the quality and the customer’s satisfaction, with which we maintain our privileged relationship around the world..

ISO  CERTIFICATE

9001:2000

ES 05/0964

Our company has NIMF 15 Certification, whose stated is to

reduce all risks due to the spread of

harmful organisms transmissible by

the wood.

䄀猀猀攀洀戀氀愀最最椀漀......................